Multi-Ornamental machine for production runs to produce wrought iron ornamental shapes by cold forming , on square, round and flat mild steel bars, profiles and tubes. Equiped with 2,5 HP (1,85 Kw) electrobrake motor and switch limit. It can also be equiped with a speed drive. All stated capacities of this machine have been based on the use of mild steel with a tensil strength of 45Kg/mm2.

Available tooling : 
Tools for producing twisting bars, simple and double baskets,scrolls, oval scrolls, folds, links, hooks, rings, balaustrade rails, bends in variable and fixed radius, bends in flat bar on edge, bends in tubes, knotts for garden fences, and railings and embossed flat bars with 13 different designs etc

Available tooling :
Tools for producing twisting bars, simple and double baskets,scrolls, oval scrolls, folds, links, hooks, rings, balaustrade rails, bends in variable and fixed radius, bends in flat bar on edge, bends in tubes, knotts for garden fences, and railings and embossed flat bars with 13 different designs.

| SOLID ROUND BAR | 10 - 20 mm. 3/8" up to 3/4" |
| --- | --- |
| SQUARE BAR | 10x10 - 20x20 mm 3/8" x 3/8" - 3/4"x3/4" |
| FLAT BAR | Up to 40x10 mm. 1 - 1/2" x 3/8" |
| TUBE | Up to Ø 42 mm.x3 mm. Ø 1 - 5/8" x 0.120" |
| FLAT TUBE | Up to 40x10 mm. 1 - 1/2" x 3/8" |
| MOTOR | 2,5 HP / 1,85 Kw. |
| VOLTAGE | 220 or 440V/ 3 Phase. |
| WEIGHT | 390 Kg. / 858 Lb. |
| SPEED DRIVE | Standard |
| NC | Optional |

| MATERIAL CAPACITIES |  |  |  |
| --- | --- | --- | --- |
| Grooved end bars (cold) | Up to 10x10mm. 3/8" x 3/8" | Up to 10mm. 3/8" | Up to 20x5 mm. 3/4" x 0.25" |
| Forged end bars | Up to 20x20mm. 3/4" x 3/4" | Up to 20mm. 3/4" | Up to 30x10mm. 1 - 1/4" x 3/8" |
| Embossed Central bars | Up to 20x20mm. 3/4" x 3/4" | Up to 20mm. 3/4" | Up to 30x10mm. 1 - 1/4" x 3/8" |

For cold forming we have to consider the tensil strength (45 Kg/mm2 maximum), the type and the diameter of the material. 
Production:
For hot forming we have to use a gas forge to get the appropiate temperature.

Plain and grooved end bars.			         Wavy end bars

Arrow points 					Embossed central bars with different designs

Pyramidal end bars

Wide end bars

Pyramidal end bars

Wide end bars