v.04-07.2016

Characteristics: Fine body filler easy to work, characterized by good shaping properties in any required thickness. Suitable hardness of putty to hardness of paintwork and the smooth non-porous surface allows to use this product as filling and finishing putty. Fill putty was designed for use on steel and glass-fibre reinforced plastics. Manual / machine sanding dry. Easy to work also with homogenous surfaces even by applying thick coats. Fill putty doesn’t fill the sanding paper. Deep imperfections are filled in a few coats. Application: The surface must be cleaned, dry, degreased and matted. Thoroughly mix putty and 2-3% of hardener BPO by weight. Apply within 5 minutes at 20oC. Higher temperature can reduce the pot life and accelerates the drying time. Note: Using too much hardener can lead to topcoat discoloration. It is not recommended to use putty below 15oC.

Technical data: VOC content: 2004/42/IIB(b)(250) <250 Fill putty CSX-01.018: Shelf-life: 12 months Density: 1,9 g/cm³ Colour: yellow Fill putty CSX-01.016: Shelf-life: 12 months Density: 1,9 g/cm³ Colour: blue Fill putty CSX-01.052: Shelf-life: 12 months Density: 1,9 g/cm³ Colour: grey

|  | Cleaning |  |
| --- | --- | --- |
|  | Hardener addition | Fill putty 100 g BPO Hardener 2-3 g |
|  | Body filling | 3 - 5 min. |
|  | Drying time | 16 - 30 min. |
|  | Hand sanding / dry | P100 - P320 |
|  | Machine sanding / dry | P100 - P320 |
|  | Store in cold place |  |