Technical specifications
ACOUSTIC STANDART METAL
Floor covering 	GPMF: 872/0	

1. Technical specifications
Issued by:	Graboplast Floor Covering Manufacturers Ltd.
	H-9023 Győr Fehérvári út 16/b.
Purpose: 	Technical data of the resilient PVC flooring with according to MSZ EN 649 sheet vinyl.

2. Application area
For use area of very heavy commercial (34) and heavy light-industrial (43) objects.
Floorcovering for commercial rooms with very heavy and for light-industrial rooms with heavy traffic.
For information on handling of the product (storing, installation, maintenance) see www.graboplast.com

3. Technical Data of the Product
Parameter	Dimension	Specification	Tolerance	Test method	
Width	cm	200; 300; 400	min.	MSZ EN 426	
Thickness	mm	2,5	+0,13; -0,10	MSZ EN 428	
Weight	g/m2	2400	+13%; -10%	MSZ EN 430	
Wear layer density 	kg/m3	1250	50	MSZ EN 436	
Dimensional stability (L/C)	%	0,2	max.	MSZ EN 434	
Curling	mm	8	max.	MSZ EN 434	
Flexibility (diameter 20/40 mm)	visual evaluation	no damage	-	MSZ EN 435	
Light fastness	grade	6	min.	MSZ EN ISO
105-B02   3. method	
Abrasion group	-	T	-	MSZ EN 660-1	
Wear layer thickness	mm	0,7	+13%; -10%	MSZ EN 429	
Castor chair	visual evaluation	no damage	-	MSZ EN 425	
Hot weld strength	N/50 mm	240	min.	MSZ EN 684	
Residual indentation 	mm	0,1	max.	MSZ EN 433	

4. Informative Data of the product 
Parameter	Dimension	Specification	Tolerance	Test methold	
Chemical resistance	visual evaluation	high resistance	-	MSZ EN 423	
Standard roll length	m	20	-	MSZ EN 426	
Slip resistance 	class	DS	-	EN 13893	
Reaction to fire	class	Cfls1	-	EN 13501-1	

Valid from:	Approved by:	
2009.06.22.	Tamás Szatmári Leader of Quality Management