## STELOXANE

## DIALANTIK
Filler to be finished with wax

# Trimetal

Technical Data Sheet

Product description

DIALANTIK is a waterborne, decorative filler based on copolymer vinyl resin, ready for use.

By the spatula-technique old appearances can be obtained which can be finished in various decorative shades by using DIALCIRE. Appropriate for interior use.

Use

DIALANTIK provides a warm and refined ambiance in various types of buildings: houses, offices, hotels, restaurants, schools, ....

DIALANTIK can be applied on all coherent and prepared interior surfaces: hydraulic mortars, concrete, plaster and derivatives, wood and derivatives, painted substrates in good condition.

DIALANTIK is a decorative filler with a matt appearance, polished or patined, which hides the irregularities of the substrate.

DIALANTIK is very durable and can be cleaned with water and sponge.

Just like wallpaper, DIALANTIK can be removed by using a steaming off-device.

Substrates

DIALANTIK can be applied indoors on a dry, healthy, coherent, non-absorbing substrate (pretreated with DIALPRIM, STELPRIM or STELATEX PRIMER INTERIOR), which is free from dust and grease.

APPLICATION OF THE FILLER:

- Is ready for use and can be applied in 1 coat on a healthy and non-absorbing substrate.

- Has to be applied by roller. Afterwards, the wet filler can be adapted with a Japanese knife, mason's float, indented spatula, effect roller, …, depending on the desired structure.

- This method will create a traditional appearance.

USE OF THE WAX DIALCIRE:

- After drying of the DIALANTIK FILLER (24 – 48 hours, depending on the film thickness) you can patine or apply the "ceruse"-technique with DIALCIRE. The wax can be applied with a cloth, brush, spalter or glove. If desired, the appearance can be faded with a soft cloth before drying of the wax.

- It contains real wax and can thus, if desired, be polished after complete drying.

- Has no tendency towards dirt collection, is scratch-resistant, washable and can be steamed off or recoated.

1/2

## DIALANTIK
Filler to be finished with wax

Practical data

Drying time at 20°C and 60 % R.H.

- Dry						After 6 hours

- Recoatable					After 24 – 48 hours (depending on the applied film thickness)

Application conditions

- Temperature of the substrate		Min. 12C

- Temperature of the environment		Min. 12C

- Relative humidity				Max. 65 %

Application and dilution

- Please revert to the previous page		Ready for use

Cleaning of tools				The filler: with water

DIALCIRE: with white spirit or SYNTHETIC THINNER

Composition

THE FILLER		DIALCIRE

- Binder(s)	Copolymer vinyl resins		Glycerol alkyd resin

- Pigment(s)	Titanium dioxide and natural fillers	None

- Solvent(s)	Water		White spirit

- Solids content	By weight: 64 + 2 %		By weight: 17 + 2 %

By volume: 44 + 3 %		By volume: 12 + 3 %

Properties

THE FILLER	DIALCIRE

- Appearance	Matt	-

- Colour	White and 7 colours by the TRIMIX-system	11 colours

- Tinting	Compatible with TRIMIX-colorants	-

- Density at 20°C	1,54 + 0,05	0,83 + 0,05

- Theoretical spreading rate	1,3 – 4 m²/l per coat	8 – 10 m²/l

(depending on the film thickness)

Shelf life

Keep frost-free.

Sheltered, 1 year in the original and unopened packaging, stored between 5°C and 35°C.

Hygiene and safety

Please revert to the Material Safety Data Sheet - please contact us in case it is not in your possession.

Keep out of the reach of children.

06/04	2/2