APPLICATIONS:Suitable for all position tungsten argon arc manual welding of pipeline. Satisfactory weiding joint can be obtained both in root pass welding and arc welding. It can also weld some low alloy steel.Such as 09Mn2Si, 16Mn, 09Mn2V and etc..

Chemical Composition of Weld Metal (%) Standard; C; Mn; Si; Cu; S; P; Re. AWS ER70S-6; 0.06-0.15; 1.40-1.85; 0.85-1.15; ≤0.30; ≤0.025; ≤0.025.

Mechanical Properties of Weld Metal Standard; Tensile Strengthбb (MPa); Yield Pointб0.2 (MPa); Elongationδ5(%); Impact V-Notch(J). AWS ER70S-6; ≥500; ≥420; ≥22; -29℃≥27.