SODIUM SILICATE SOLID

CHEMICAL NAME: Sodium silicate ( Na2O x n SiO2 )

MANUFACTURING PROCESS: Silica sand melting with soda ash

| Technical data | UM | Value |  |
| --- | --- | --- | --- |
|  |  | Type 1/3 | Type 1/2 |
| Appearance | - | glassy granules | of 8 - 10 cm |
| Colour |  | blue, green, | brown |
| SiO2 content | % | 72 - 76.5 | 62 - 67 |
| Na2O content | % | 21.5 - 25 | 31 - 36 |
| Metal oxides (R2O3) content | % | 2.6 | 1.9 |
| CaO content | % | 1.1 | 1.1 |
| Modulus (SiO2/Na2O) |  | 3.0 - 3.7 | 1.8 - 2.2 |

APPLICATION:

Preparation of liquid sodium silicate.

PACKING AND STORAGE:

In 1000 kg big bags or in bulk.

HANDLING:

The product does not require any special cautions.

STORAGE:

In clean, specially arranged areas.

GUARANTEE PERIOD:

The product is guaranteed for 12 months, providing that packaging, conveyance and storage provisions are observed.